## Slide 1
Cathodic corrosion - a quick, clean and versatile method for the synthesis of metallic nanoparticles
The essence of corrosion
A. Yanson

## Slide 2
Electrochemical measurement - voltammogram
Common corrosion is anodic, it always proceeds via oxidation of a metal to its cation:
Pt ↔ Pt2+ + 2 e− (+1.19 V)
Fe ↔ Fe2+ + 2 e− (-0.44 V)
Zn ↔ Zn2+ + 2 e− (-0.76 V)
If making metal more positive speeds up corrosion, making it more negative …
-1 -0.8 -0.6 -0.4 -0.2 0 Potential applied (V)
Corrosion of a screw in sea water
reduction
oxidation
anodic
cathodic
equilibrium (red-ox) potential
Current

## Slide 3
Cathodic protection
Cathodic protection - galvanic
To keep an easily oxidizable metal from corroding we need to constantly “feed” it with extra electrons, either from external power supply or by corroding a sacrificial anode:
What will happen if we take a platinum electrode and make it a cathode?

## Slide 4
Scanning Tunneling Microscope (STM) needs an atomically sharp tip made of a very stiff and chemically inert metal
W etching in NaOH:
STM tip etching

## Slide 5
A literature recipe for Pt-Ir tip etching:
- seems to work just fine, doesn’t it?
- but 50Hz is so boring! Let’s use a function generator and see how frequency influences the etching process
AC high voltage PtIr etching

## Slide 6
The case of zero frequency (water electrolyis):
Cathodic treatment of a Pt wire at -10V in 10M NaOH
99.99% Pt
 0.1mm

## Slide 7
Cathodic treatment of Pt (10M NaOH, -10V, 1000 sec)
before
Surface area increase x17
Cyclic voltammogram of Pt in H2SO4
SEM images of electrode surface
Yet another way to make platinum sponge?
Or does this look like nanoparticles?!
after

## Slide 8
0.5 M
1 M
5 M
10 M
20 M
Pt wire after 10 minutes of cathodic treatment at -6 ± 0.5 V in NaOH
Cathodic corrosion of Platinum (?!)

## Slide 9
So what’s going on?
Nanoparticles (or so it seems)
Cathodic corrosion of platinum
Ingredients: Pt, C, Na, H, O, (negative pole!)
This is NOT what we observe!!!
Cathodic protection vs. cathodic corrosion

## Slide 10
Surely someone must have seen this before?
Most popular explanations:
Alloying with reduced alkali metal and subsequent leaching by water
Hydrogen corrosion (formation of metal hydrides)
Physical disintegration
Historical note

## Slide 11
Alloying of a cathode metal with an alkali, and subsequent leaching of the alloy is inconsistent with the following observations: At one given potential the alkali cation shows preference both for reduction (alloying) and for oxidation (leaching) Na+ + e− ↔ Na(s) (-2.71 V) At more cathodic potentials leaching should be suppressed completely.
Haber’s mechanism: alloying+leaching

## Slide 12
TMAH -10 to 0 Vac
TMAH -10Vdc
It can’t be alloying! But how do you prove it?
Idea: use a strong base which does not have an alkali

## Slide 13
Most popular explanations:
Alloying with reduced alkali metal and subsequent leaching by water
Hydrogen corrosion (formation of metal hydrides)
Physical disintegration
Idea: start with an acid, then add an alkali salt of the same acid
Why this should work: conductivity, heat conductivity, density and all other physical properties
will remain the same (approx.). Chemically, the only thing we add is alkali cation.
Let’s see what that will do…
It can’t be alloying! But how do you prove it?
The case of tetra-alkyl ammonium cations

## Slide 14
Most popular explanations:
Alloying with reduced alkali metal and subsequent leaching by water
Hydrogen corrosion (formation of metal hydrides)
Physical disintegration
It can’t be alloying! But how do you prove it?
-10 V in 2M H2SO4
After annealing
-10 V in 1M H2SO4+ 1M Na2SO4
Strong cation is key

## Slide 15
It’s not hydrogen, and also not physical disintegration
Au wire after 30 min at -10 V in 1M H2SO4 (left), and after 1M Na2SO4 was added (right).
Most popular explanations:
Alloying with reduced alkali metal and subsequent leaching by water
Hydrogen corrosion (formation of metal hydrides)
Physical disintegration
Strong cation is key

## Slide 16
To summarize, in order to cathodically corrode a metal, we need:
a metal
a strong cation in aqueous solution
quite negative voltage
and thus the proposed mechanism of the reaction …
… the reaction must proceed via a negatively charged metal ion!
Yanson et al, Angewandte 50, 6346 (2011)

## Slide 17
This is known:
etc etc etc
This is waiting
to be
discovered!

## Slide 18
History of metal anions
What is known of metal anions
In 1907 experiments in liquid ammonia by Kraus produced species of Na+ and Pb2-
In the 1930’s Zintl deduced the existence of Na4Pb9, or a “Zintl ion” Pb94-. Also detected anion Au-
By the end of 1940’s anions of Hg-, Au- and Li- were identified in gas phase by mass-spec
In the 1950’s the first solid ionic compounds of the type Cs+Au- were synthesized in vacuum
In 1980’s unambiguous evidence appeared for the existence of monatomic metal anions in solution and the solid state
In 2003 a Cs2Pt solid containing Pt2- anion was obtained
Ge94-
Cs4Ge9

## Slide 19
… they exist, but are hard to find and handle (intolerant to air, water, anything reducible)
Low-temperature STM of Au atoms on NaCl
J. Repp, G. Meyer, F.E. Olsson, and M. Persson, Science 305, 493 (2004)
An example of a gold anion from physics

## Slide 20
In 1907 experiments in liquid ammonia produced species of Na+ and Pb2-
In the 1930’s Zintl deduced the existence of Na4Pb9, or a “Zintl ion” Pb94-. Also detected anion Au-
By the end of 1940’s anions of Hg-, Au- and Li- were identified in gas phase by mass-spec
In the 1950’s the first solid ionic compounds of the type Cs+Au- were synthesized in vacuum
In 1980’s unambiguous evidence appeared for the existence of monatomic metal anions in solution and the solid state
In 2003 a Cs2Pt solid containing Pt2- anion was obtained
Onset potential for Pt is less negative than -2V !
Ge94-
Cs4Ge9

## Slide 21
How does the corrosion product look like?
Characterization of cathodic nanoparticles

## Slide 22
TEM
Characterization of cathodic nanoparticles
EDX
XRD
0
20
40
60
80
100
120
140
160
180
200
0-2
2-4
4-6
6-8
8-10
10-12
12-14
14-16
16-18
18-20
20-22
22-24
More
nm
Size distribution
Physical characterization

## Slide 23
Catalytic activity of cathodic platinum nanoparticles
Black – commercial (TKK) 5 nm
Red – cathodic platinum 8-10 nm
Hydrogen adsorption
CO monolayer oxidation
Methanol oxidation
Fuel cell performance of CathNP

## Slide 24
Pd cathodic nanoparticles
M. Hara et al. / Electrochimica Acta 52 (2007) 5733–5748
Single crystal Pd data for reference (10mV/sec)
(111)
(100)
(110)
Blank voltammetry of Pd CathNP

## Slide 25
Rh cathodic nanoparticles
Q. Xu et al. / Electrochimica Acta 54 (2009) 5509
Single crystal Rh data for reference (1mV/sec)
(111)
(100)
(110)
(100) or (110)
Blank voltammetry of Rh CathNP

## Slide 26
Powder X-ray diffraction:
2-1-2 peak sequence is typical of fcc metal crystals
Positions of the peaks coincide with those expected for the crystal structure of a corresponding metal
Widths of the peaks give indication for the average crystallite size to be 25, 58, 12, 57 and 6 nm, respectively (Scherrer formula).

## Slide 27
We have confirmed the ac formation of suspended nanoparticles for Pt, Au, Cu, Ag, Ni, Rh, Re, Al, Ti, Si, Nb and Ru - in fact every metal we have tried (except Pd)
Any electrolyte works, any pH, as long as it has a strong cation
Any electrolyte, any metal
Pt
Au
Rh
Ag
Re

## Slide 28
… what if the starting wire is an alloy?
EDX analysis
of nanoparticles
… then we get alloyed nanoparticles!
Rodriguez, Yanson, JACS 133, 17626 (2011)

## Slide 29
Electrochemistry of PtRh NPs
Pt
Pt90Rh10
Pt70Rh30
Pt20Rh80
Rh
Blank CV
CO stripping
Methanol
oxidation
0.5M H2SO4 + 0.5M
CH3OH, 20 mV/sc
Pt (-----)
Pt90Rh10 (-----) Pt70Rh30 (-----)
Pt20Rh80 (-----)
Rh (-----)
0.5M H2SO4 +
0.1M NaNO3, 20 mV/s
Nitrate
reduction
Rodriguez, Yanson, JACS 133, 17626 (2011)

## Slide 30
Electro-oxidation on cathodic Pt95Ru5 nanoparticles
0.5M H2SO4 + 0.5M CH3OH, 20 mV/sc
CO stripping
Methanol oxidation
Rodriguez, Yanson, JACS 133, 17626 (2011)

## Slide 31
Size-controlled synthesis of cathodic nanoparticles
We can simply control the size of the cathodic NPs,
without sacrificing size distribution
Antonov, Yanson , Electrochim. Acta 110, 796 (2013)

## Slide 32
NH3 oxidation
0.2M NaOH + 0.1M NH3
10 mV/s
0.5 M H2SO4, 50 mV/s
% (100) sites
59% -----
55% ----- 35% -----
31% -----
DME oxidation
Preferentially-oriented Pt(100) nanoparticles

## Slide 33
0.1M NaOH +2mM NaNO2, 1 mV/s
Nitrite reduction to N2 on cathodic Pt(100) nanoparticles
Duca, Yanson , Topics in Catalysis 57, 255 (2014)

## Slide 34
Prof. M. T. M. Koper
Dr. Matteo Duca
Dr. Yuriy Yanson
Rik Mom
Rico Wanders
Pavel Antonov
Prof. Oosterkamp (SEM)
Prof. Reedijk (XRD)
Leiden University
Dr. Paramaconi Rodriguez, Paul Scherrer Institute & University of Birmingham
Dr. Nuria Garcia,
University of Southampton
Prof. N. Markovic
Argonne National Lab
Prof. P. Unwin
Dr. S. Lai
University of Warwick
Dr. Frans Tichelaar (TEM, EDX)
Dr. Patricia Kooyman (TEM)
TU Delft

## Slide 35
Facile preparation of Pt hydrosols by dispersing bulk Pt with potential perturbations
Wei Huang, Shu Chen, Jufang Zheng, Zelin Li, Electrochemistry Communications 11 (2009) 469
Reference discovered accidentally during an irrelevant literature search on 31-05-2011
… unaware, we wrote an article (published online 27-05-2011) and applied for a patent

## Slide 36
Stability of cathodic Pt(100) nanoparticles